Wall painting conservation

Pieta Greaves (Courtesy of Tom Guderjan/Maya Research Program)

Introduction

Excavated in 2013, the room which the wall painting in located is in a vaulted room of Structure 2 (figure 2), which is part of a partially excavated building complex (ref 2013 excavation report). The room was filled with large uncut stones at the beginning of the late classic and the room was sealed. Areas of the original room have now collapsed and room is protected by wooden roof and tarpaulin (figure 2) which also extends over the doorway to protect the wall painting from the climatic conditions.

Figure 1: External view of Structure 2

Figure 2: current roof construction

Condition assessment

The wall painting is 6 x 2 in size (figure 3), the plaster once extended across the whole back wall but due to losses over time the back wall cut stones are visible in some areas. Two layers of plaster are visible both with painted details (figure 4), an older layer one and a newer layer two, the lower plaster level is further decorated with red and orange pigment, it cannot be determined if this is a simple or elaborate design.

Figure 3: View of wall painting through doorway

Lower layer of plaster

Upper layer of plaster

Figure 4: upper and lower plaster layers with pigments visible

The plaster is applied onto large cut blocks which form the back wall of the room, a doorway on the North side had been blocked with further cut blocks prior to the application of the first layer of plaster. The wall painting does not extend all the way to the roof, but stops as the wall begins to angle at 2m in height from the bench (figure 5).

Height of plaster

Figure 5: height of plaster wall in Structure 2

On inspection of the wall painting in June 2014 it is clear that the much of the wall painting design has not been retained due to the environment and soluble nature of both the pigments and the plaster, there are small sections of design that can be seen, but the images cannot be clearly made out. Areas where details of the original painting survive are very small and the largest is no bigger that 10cm x 10 cm. The majority of the decorations seems to have been concentrated on the central area of the wall, however very small and isolates areas of red colour can be seen at either end of the wall, perhaps indication that at the very least the walls were partially coloured at the sides. The pigments are assumed to be naturally occurring ochres, however further test are required. The images are only fragmentary and require a specialist to further determine the nature of the images.

Much of the surface appeared fragile in nature with several sections which are not becoming detached from the stone cut blocks of the wall, small sections of the identifiable painted designs on the top layer of plaster and were no longer secure to the substrate and moved when touched. Areas that appear uneven are due to the movement of the plaster over time due to the high humidity and possible water ingress. Also the plaster suffers from root damage which has led to loss of surface and distortion.

The surface of the wall painting was covered in decayed plaster, re-deposited calcium carbonate/sulphate from the plaster itself interacting with the water in the environment and bat droppings from bats which now inhabit the room.

There are areas of burnt plaster in the middle base section of the wall painting (figure 6), this has caused a small crust on the surface of the wall painting and interestingly some of the layer 1 plaster has also been burnt indicating that this area was already in a state of decay and the top layer had already suffered from losses when the burning took place.

Plaster layer 2 burnt by fire

Plaster layer 1 burnt by fire

Figure 6: Blackening of both top and bottom layers

Along with the previously identified areas of painted plaster, eleven areas were identified with racking light that contained crude graffiti, (figure 7) scratched into the surface, although mostly unidentifiable in nature, deliberate shapes and forms could be made out. The graffiti has been carved into multiple areas and into both the top and bottom layers of plaster further indicating the poor state of the top layer when buried.

Figure 7: graffiti #8 with design extending on both the top and bottom plaster layers

The graffiti is further discussed at the end of this report.

Conservation

Simple conservation techniques were carried out on site, due to the size and condition of the wall painting, it was decided to preserve in-situ as moving could cause damage.

As the greatest threat to the wall painting was loss due to plaster crumbing, consolidation was conducted prior to any cleaning of the surface.  Loose or moving areas of wall painted were consolidated with 10 % Paraloid B72 (poly methyl-methacrylate/ethacrylate copolymer), applied with a syringe. The edges where also consolidated as cohesion between the plaster and the wall are week. In some areas the consolidant has darkened the area but this will add stability to the very fragile areas so the benefit outweighs the aesthetics.

Solvent tests on the pigments showed that the pigments were very soluble in acetone but less so in water, which would remove the excess plaster and dirt from the surface. Following swabbing of the surface with cotton buds and bottled water small areas of paint became more visible, the graffiti was more defined as the re-deposited calcium carbonate/sulphate was removed from the grooves.

The bat droppings were difficult to remove without loss to the wall pigments, some was left of the wall where it was felt that there was a risk of removing painted details. Consideration was given to the idea of removing some of the plaster from the top layer to investigate whether the lower layer painting was identifiable, however with the discovery of the graffiti and the unknown state of preservation of the lower pigment layers it was felt that this was too greater risk.

Roots were removed were they would not pose any risk of loss to the plaster, any large roots were consolidated with Paraloid B72 so to secure any loose plaster.

Graffiti

The thickness of the lines are variable, but none are thicker than 2mm. The freehand style of the designs allows for the observation to determine directionality of the line drawn where the line thins at the end of each stroke. Due to the hardness of the plaster and the cleanness of the lines, it is likely that a lithic tool would have been used to create the designs. Graffiti was labelled numbers 1-11 as discovered, and are photographed and illustrated below, Illustration 3 maps the location of the graffiti on the western wall.

Graffiti # 1 and  # |2: unknown animal and fish

Graffiti # 3 and Graffiti # 4

Graffiti  # 5

Graffiti#  6 and Graffiti # 7: A connected scene of a crouched figure looking over the sun towards a monster?

Graffiti # 8

Graffiti # 9: An unknown amount of the Graffiti is missing due to plaster loss.

Graffiti # 10

Graffiti  # 11: no longer attached to wall due to failure of the plaster.